Controlled Cobalt Doping in Biogenic Magnetite Nanoparticles

Byrne, J M; Coker, V S; Moise, S; Wincott, P L; Vaughan, D J; Tuna, F; Arenholz, E; van der Laan, G; Pattrick, R A D P; Lloyd, J R; Telling, N D (2013)

Accepted for publication in Journal of The Royal Society Interface

The data contained within this dataset is arranged according to the measurement technique used to collect each file. Details of the files are outlined below.

SLP (Specific loss power)

4 datasets labeled “CoX_87kHz” where X = %Co, containing four columns corresponding to:

Time(s)

Temperature (°C)

Temperature increase (°C)

Temperature increase (°C/g Fe) – Calculated as a function of the mass of iron in the sample

Moessbauer

12 files labeled “CoX_Y”, where X = %Co and Y = LT or RT (Low temperature or room temperature). Each file contains columns corresponding to:

v (mm/s) – Velocity

Data – Raw data collected using Moessbauer

Icalc – Calculated fit of the data, i.e. sum of the individual component fits

Sextets or Doublets – Individual component fits

SQUID (Superconducting Quantum Interface Device)

18 files labeled “CoX_Hys5K” – hysteresis loops collected at 5K, “CoX_Hys300K” – hysteresis loops collected at 300K and, “CoX_ZFC_FC_REM_100G” – zero field cooled (ZFC), field cooled (FC) and remanence (REM) collected under a field of 100 Gauss. X = %Co. All data files are arranged in the columns:

Field (Oe) – Magnitude of the applied magnetic field in Oersteds

Temperature (K) – Temperature of measurement

Long Moment (emu) – Magnetic moment measured by the SQUID

M(emu/g) – Calculated magnetization as a function of the long moment per gram of sample

XMCD (x-ray magnetic circular dichroism)

17 files labeled “CoX_FeEdge” – XAS (x-ray absorption) collected on the iron L edge, “CoX_CoEdge” – XAS collected at the cobalt L edge, “CoX_FeEdge_Fit” – calculated fit of the iron edge XMCD. X = %Co.

XAS data arranged in columns:

eV – Beamline energy

XAS+ - XAS collected under positive magnetic field (+0.6T)

XAS- - XAS collected under negative magnetic field (-0.6T)

XMCD – Difference between XAS+ and XAS-

Lin.XAS – Average of XAS+ and XAS-

Lin.XAS-Step – Redundant column

Integ.XAS – Redundant column

Integ.XMCD – redundant column

XMCD data arranged in columns:

eV – Beamline energy

Raw data – Obtained from difference between XAS+ and XAS-

Component data (Fe2+[B]) – Fit of Fe2+ octahedral site

Component data (Fe3+(A)) – Fit of Fe3+ tetrahedral site

Component data (Fe3+[B]) – Fit of Fe3+ octahedral site

Fit – Sum of the three component fits

XRD (X-ray diffraction)

1 File containing all X-ray diffraction patterns. Arranged in columns:

CoX – Angle (2theta), X = %Co

Intensity (Arb. Units) – Intensity of the recorded signal